Technical datasheet

What is the porcelain specification?

Porcelain / Ceramic Specification: Premium Handmade High-Relief 3D Designer Tiles (Crafted with high-strength body/glaze). Both Cermaic & Porceline body available.

Water absorption?

< 0.5% (Vitrified Body) / < 3% (High-density Decorative Ceramic Body).

Frost resistance?

Yes 100% Frost Resistant. (Suitable for both indoor and covered outdoor feature walls).

Slip resistance?

Not Applicable (Designed primarily for vertical wall cladding & high-relief feature surfaces). Easy to clean and maintain.

Exterior suitability?

Yes, highly suitable for elevation, accent walls, and exterior facade cladding. Resistant to all types of weather.

UV resistance?

100% UV Resistant (Special lightfast glazes; colors and metallic accents will not fade or discolor under direct sunlight).

Chemical resistance?

Resistant to normal household cleaners, mild acids, and non-abrasive detergents.

Pool suitability?

Suitable for outdoor feature walls / water feature backdrops near pool areas (Not recommended inside active pool tanks due to 3D surface depth).

PEI rating?

Surface Hardness: Surface hardness Mohs 5-6 (High scratch resistance for wall applications).

Thickness?

8mm to 9mm

Weight?

Depends on size. Will be mentioned in packing list

Installation method?

High-bond Polymer-Modified Tile Adhesive (Class C2TE standard). Mechanical anchoring/dry cladding recommended for high-rise exterior installations.

Grout recommendations?

Epoxy Grout or Non-shrink Polymer Grout with a minimum 2–3 mm tile spacer to accommodate 3D edge alignment.

Maintenance?

Easy to clean with a soft brush, micro-fiber cloth, or standard mild detergent. Non-porous glazed finish prevents dust buildup

Lead/cadmium compliance?

100% Lead & Cadmium-Free (Non-toxic, eco-friendly glazes compliant with safety norms).

Fire characteristics where applicable?

Class A1 Fire Rated (100% Non-combustible, zero flame spread, no smoke emission).

Country of origin?

Made in India

Size options as single piece?

- 20cm x 20cm / 7.87  x 7.87 inches

- 30cm x 30cm – 11.80 x 11.80 inches

- 60cm x 60cm – 23.60 x 23.60 inches / 2 feet x 2 feet

- 90cm x 60cm – 2.95  x 2 feet

- 160cm x 80cm – 5.25 x 2.60 feet

- 120cm x 60cm – 3.93 x 2 feet

- 240cm x 120cm – 7.87 x 3.93 feet