Technical datasheet 
What is the porcelain specification?
Porcelain / Ceramic Specification: Premium Handmade High-Relief 3D Designer Tiles (Crafted with high-strength body/glaze). Both Cermaic & Porceline body available.
Water absorption?
< 0.5% (Vitrified Body) / < 3% (High-density Decorative Ceramic Body).
Frost resistance?
Yes 100% Frost Resistant. (Suitable for both indoor and covered outdoor feature walls).
Slip resistance?
Not Applicable (Designed primarily for vertical wall cladding & high-relief feature surfaces). Easy to clean and maintain. 
Exterior suitability?
Yes, highly suitable for elevation, accent walls, and exterior facade cladding. Resistant to all types of weather. 
UV resistance?
100% UV Resistant (Special lightfast glazes; colors and metallic accents will not fade or discolor under direct sunlight).
Chemical resistance?
Resistant to normal household cleaners, mild acids, and non-abrasive detergents.
Pool suitability?
Suitable for outdoor feature walls / water feature backdrops near pool areas (Not recommended inside active pool tanks due to 3D surface depth).
PEI rating?
Surface Hardness: Surface hardness Mohs 5-6 (High scratch resistance for wall applications).
Thickness?
8mm to 9mm
Weight?
Depends on size. Will be mentioned in packing list

Installation method?
High-bond Polymer-Modified Tile Adhesive (Class C2TE standard). Mechanical anchoring/dry cladding recommended for high-rise exterior installations.
Grout recommendations?
Epoxy Grout or Non-shrink Polymer Grout with a minimum 2–3 mm tile spacer to accommodate 3D edge alignment.
Maintenance?
Easy to clean with a soft brush, micro-fiber cloth, or standard mild detergent. Non-porous glazed finish prevents dust buildup
Lead/cadmium compliance?
100% Lead & Cadmium-Free (Non-toxic, eco-friendly glazes compliant with safety norms).
Fire characteristics where applicable?
Class A1 Fire Rated (100% Non-combustible, zero flame spread, no smoke emission).
Country of origin?
Made in India
Size options as single piece?
· 20cm x 20cm / 7.87  x 7.87 inches
· 30cm x 30cm – 11.80 x 11.80 inches
· 60cm x 60cm – 23.60 x 23.60 inches / 2 feet x 2 feet
· 90cm x 60cm – 2.95  x 2 feet
· 160cm x 80cm – 5.25 x 2.60 feet
· 120cm x 60cm – 3.93 x 2 feet 
· 240cm x 120cm – 7.87 x 3.93 feet


